Industrial Laser Cutter
Pro Tips
This is not an exhaustive list, but there are a few tips for achieving a better surface finish. Some experimentation may be required, but a quite good surface finish is possible with some setup and care.
Cast acrylic leaves a better surface finish and less deformation than extruded acrylic. If surface finish is important, use cast acrylic.
Higher pressure air assist removes residue from work piece more efficiently and leaves a better surface finish with less post-processing. If available, using an air compressor to feed the air assist will provide a better surface finish.
Flashback (reflections from the holders that scar the back of the work piece) can cause residue to form on the back/bottom of work piece. Consider using the “Slats” or a “pin bed” to hold the work piece in order to reduce flashover and leave a better surface finish on back.
When etching glass, the 150W lasers are usually too powerful. Use a low power setting and consider de-focusing the beam slightly. Also, applying a thin layer of dilute dish soap to work piece to facilitate cleaning of small glass particles formed during etching process.